Standard PolyDrain – 2611

Precast Polymer Concrete Catch Basin w Ductile Iron Frame and Grate

Standard Specification

System ID#: PD 2611

Trench drain shall be PolyDrain; manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC - (800) 438-6057. www.abtdrains.com

System Components:

Precast Catch Basin - The precast catch basin shall be manufactured using polyester polymer concrete with the following material properties when tested:

Property			    Test Method			Value

Compressive Strength 		    ASTM C579 			14,000 psi Minimum

Bending Strength 		    ASTM C580			4,000 psi Minimum

Tensile Strength 			    ASTM C307			2,000 psi Minimum

Moisture Absorption		    ASTM   D570			0.1% Maximum

Chemical Resistance		    ASTM C267 			Pass

Freeze/Thaw w/o weight loss 	    ASTM C666			1600 Number of Cycles Minimum

Resistance to Fungi 		    ASTM G21			Zero (0) Rating Mold Growth

UL/ULC Listed- Flame Spread 	    UL-723			Class A

The catch basin consisting of 3 sections:  top with frame and grate; middle section; and closed bottom section with nominal 19” (483mm) x 12” (300mm) inside width.

Frame & Grate: #603/604- Black polymer coated ductile iron conforming to ASTM A-536 with a minimum of 0.21Ft2 /L Ft (.064m2/Lm) open area. Grates shall meet a minimum 620 psi proof load per AASHTO M-306 test.  Frames shall be independent of the channels. Frames and grates shall seat into basin without rocking and shall be bolted at all four corners.  Frames and grates shall be made in U.S.A., and shall conform to the FHWA's "Buy America" policy 23 CFR 635.410(b) and Federal Acquisitions Regulations (FAR) 52.225 “Buy American Act”.

Quality Assurance:

Submittals:  A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer. Grates shall be independently tested to AASHTO M-306.